Wavelength dispersive scan of oxygen K and Zn L (2nd order) showing proper correction for refractive index. 15 keV, ZnO standard.

# BRAGG'S LAW

In 1913, the father-son team of William H + William L Bragg built an X-ray spectrometer, using NaCl to resolve Pt X-rays. For this they received the Nobel Prize in 1915.

where :			is the order of the x-ray (1st, 2nd, etc.)

is the wavelength in angstroms

is the analyzing crystal 2d spacing in angstroms

is the angle of diffraction

There is a more precise form of Bragg's Law that allows for refraction of x-rays by the crystal or diffractor; this can be shown as a modification of the 2d such that d' = d[1-(k/n2)] where n is the order of reflection and k is a constant for each crystal. These constants range from 6x10-5 for LiF to 2.2x10-3 for TAP (Reed, 1993). They can cause higher order lines to "cross over" and appear on the opposite side of a peak, such as the 3rd order P Ka upon the F Ka for LDEs. Probe for Windows automatically uses this more accurate form of the calculation.