Attempt to calculate “density” of oxygen in oxide compounds for use in Thin Film calculations (StrataGem assumes gaseous density for density calculations which is not realistic).

Oxygen, oxide density

| Oxide | Compound oxide density | Cation | Cation “density” (assume elemental) | Anion (oxygen) | Calculated oxygen “density” in compound |
| --- | --- | --- | --- | --- | --- |
| MgO | 3.58 | Mg | 1.74 | O | 5.42 |
| SiO2 | 2.20 | Si | 2.34 | O | 2.13 |
| ZnO | 5.61 | Zn | 7.17 | O | 4.08 |
| TiO2 | 4.26 | Ti | 4.5 | O | 4.14 |
| Cr2O3 | 4.26 | Cr | 7.19 | O | 3.90 |

Example for ZnO:

(7.14 + x))/2 = 5.61

x = 4.08

Example for SiO2:

(2.34 + 2x)/3 = 2.20

x = 2.13

John Donovan

Univ of Oregon